The winter-protecting cloth fabric specifications

1.       Fabric fiber composition (ISO 1833-1:2006) >51% cotton;

2.       Antistatic, according to EN1149-3 standard (for electrical staff);

3.       Fabric weight (ISO 3801:1977) 250 - 300 g/m2;

4.       Internal warming material (“Sintifon”) - gray, 150 gr/m2;

5.       Color sustainability to light (ISO105-B02:1994) >4;

6.       Color sustainability to washing (ISO105-C06:2010), color change >4;

7.       Water resistance: (AATCC100) according to ISO 4920 standard 4 or 5;

8.       Tearing strength (N/5 cm) (ISO13934-1 enamel method CRE); Main >800, secondary >400;

9.       For sewing, use reinforced polyester thread of size 40/3 and 30/2;

10.   The tearing load of seams should be - not less than 250 N;

11.   Zipper fasteners of sizes 5 to 7 made of hard, durable, polymer material;

12. Signal belt – grey – 3 cm (for night vision)

13. Signal belt – two colored (grey and green) – 5 cm (for night and day vision)

The fabric specifications for T-shirts

1.       Fabric fiber composition (ISO 1833-1:2006) is nearly 96% cotton;